__________________________________________________________________________________________

Toll Free: (888) 833-8308								Durajoint Concrete Accessories

Fax: (330) 527-2440 										10426 Industrial Drive

Web: www.durajoint.com									Garrettsville, OH 44231

Ribbed with Centerbulb Waterstop

Type 13

Weight: (lbs/ft) 1.59	______ ________________________

Width: 6”				                            _______

Thickness: 3/8” Flare	____	Head Pressure: (Ft)   200_

Typical Properties

CRD-C 573: 	Tensile Strength 1925 psi – 13.3 MPa

CRD-C 573: 	Ultimate Elongation 402%

CRD-C 571: 	Stiffness in Flexure 775 psi

ASTM D-624: 	Tear Resistance 380 lbs. /in.

ASTM D-1149	Ozone Resistance passed

CRD-C 570: 	Low Temperature - No Cracking, Brittleness (-35°F) or Splitting

CRD-C 572: 	Accelerated Extraction

Ultimate Elongation 366% Par 7.1

Tensile Strength 1825 psi Par 7.1

CRD-C 572: 	Effects of Alkalies Loss in Weight

0.10% Max. Par 7.2

Gain in Weight 0.25% Max.

1/4”

1/2”

12”

3/16”

7/8 ID & 1-1/2” OD

Waterstop • Forming Accessories • Rebar Supports • Mesh Supports • Prestressed Accessories