__________________________________________________________________________________________

Toll Free: (888) 833-8308								Durajoint Concrete Accessories

Fax: (330) 527-2440 										10426 Industrial Drive

Web: www.durajoint.com									Garrettsville, OH 44231

Post Applied Durajoint Type 18 TPER Kit

All waterstop shall be Durajoint PVC Waterstop as manufactured by Durajoint.

It shall be an extrusion of chemically resistant thermal elastomeric rubber and additional

resins, plasticizers and stabilizers which meet or exceed the requirements of the

Corps of Engineers specifications. Types and dimensions of waterstop shall be

those shown in the project specifications.

Typical Properties

ASTM D-412: 	Tensile Strength Min. 1800 psi                   ASTM D-412: Ultimate Elongation Min. 450%

ASTM D-624: 	Tear Resistance 278 lbs. /in.                      ASTM D-2240	Hardness Max. 80 min.

ASTM D-792	Specific Gravity 0.96 min.                           ASTM D-570	Water Absorption Max. 0.15%

ASTM D-1171	Ozone Resistance 450                               ASTM D-412	100% Modulus 1000 psi                                     ASTM D-746

1/4”

1/2”

12”

3/16”

7/8 ID & 1-1/2” OD

: 	Low Temperature - No Cracking, Brittleness (-75°F) or Splitting

Description:

Post Applied Durajoint was created to enable to attach a new concrete structure to an existing concrete structure, providing a water tight joint.

Application:

Surface of concrete where Post Applied Durajoint will be placed, must be smooth and sound. Beads of Durajoint RTV 7500 Silicone should be applied to the concrete surface near to the anchor bolts in full length.

Place the Post Applied Durajoint into the desired position, then fasten by using the anchor bolts and the stainless steel bars as supplied by Durajoint Concrete Accessories.

Placement: Batten Bar side edge should be placed ½” in from edge of waterstop.

Each kit contains: 2) -Stainless Steel batten bars measuring 10’ x 1” x 1/8” –Each Bar has 20 pre-drilled placement holes along the length of the bar.

40)- Stainless Steel Anchors (1/4” x 2-1/4”) and Anchor Bolts.

Waterstop • Forming Accessories • Rebar Supports • Mesh Supports • Prestressed Accessories