__________________________________________________________________________________________

Toll Free: (888) 833-8308								Durajoint Concrete Accessories

Fax: (330) 527-2440 										10426 Industrial Drive

Web: www.durajoint.com									Garrettsville, OH 44231

Ribbed with Centerbulb Waterstop

Type 4

Weight: (lbs/ft) .89	                      I.D. Diameter: 3/16”_____

Width: 6”				O.D. Diameter: 1/2”_____

Thickness: 3/16” 			Head Pressure: (Ft)   100_

All waterstop shall be Durajoint TPER Waterstop as manufactured by Durajoint.

It shall be an extrusion of chemically resistant thermal elastomeric rubber and additional

resins, plasticizers and stabilizers which meet or exceed the requirements of the

Corps of Engineers specifications. Types and dimensions of waterstop shall be

those shown in the project specifications.

Typical Properties

ASTM D-412: 	Tensile Strength Min. 1800 psi

ASTM D-412: 	Ultimate Elongation Min. 450%

ASTM D-624: 	Tear Resistance 278 lbs. /in.

ASTM D-2240	Hardness Max. 80 min.

ASTM D-792	Specific Gravity 0.96 min.

ASTM D-570	Water Absorption Max. 0.15%

ASTM D-1171	Ozone Resistance 450

ASTM D-412	100% Modulus 1000 psi

ASTM D-746

1/4”

1/2”

12”

3/16”

7/8 ID & 1-1/2” OD

: 	Low Temperature - No Cracking, Brittleness (-75°F) or Splitting

Waterstop • Forming Accessories • Rebar Supports • Mesh Supports • Prestressed Accessories