Toll Free: (888) 833 8308				         Durajoint Concrete Accessories                                                                                                                                                 Fax: (330) 527 2440  					           10426 Industrial Drive                                                                                                                                                                         Web: www.durajoint.com					        Garrettsville, OH  44231

Ribbed Type with Centerbulb

Durajoint Type 5 TPER

Weight: (lbs/ft) 1.14                                                                     Centerbulb I.D. 3/8”  O.D.: 5/8”

Width: 6”                                                                                                                                        .

Thickness: 3/8”                                                                                           Head pressure: (Ft) 125

All waterstop shall be Durajoint PVC Waterstop as manufactured by Durajoint.

It shall be an extrusion of chemically resistant thermal elastomeric rubber and additional

resins, plasticizers and stabilizers which meet or exceed the requirements of the

Corps of Engineers specifications. Types and dimensions of waterstop shall be

those shown in the project specifications.

Typical Properties

ASTM D-412: 	Tensile Strength Min. 1800 psi

ASTM D-412: 	Ultimate Elongation Min. 450%

ASTM D-624: 	Tear Resistance 278 lbs. /in.

ASTM D-2240	Hardness Max. 80 min.

ASTM D-792	Specific Gravity 0.96 min.

ASTM D-570	Water Absorption Max. 0.15%

ASTM D-1171	Ozone Resistance 450

ASTM D-412	100% Modulus 1000 psi

ASTM D-746

1/4”

1/2”

12”

3/16”

7/8 ID & 1-1/2” OD

: 	Low Temperature - No Cracking, Brittleness (-75°F) or Splitting

Waterstop      Forming Accessories       Rebar Supports      Mesh Supports      Prestressed Accessories