__________________________________________________________________________________________

Toll Free: (888) 833-8308								Durajoint Concrete Accessories

Fax: (330) 527-2440 										10426 Industrial Drive

Web: www.durajoint.com									Garrettsville, OH 44231

Ribbed with Centerbulb Waterstop

Type 7F

Weight: (lbs/ft) 3.01		_____  I.D. Diameter: 1 1/2”______

Width: 9”				O.D. Diameter: 2 1/4”_____

Thickness: 3/8” -3/16” 		Head Pressure: (Ft)   150+_

All waterstop shall be Durajoint PVC Waterstop as manufactured by Durajoint.

It shall be an extrusion of virgin polyvinyl chloride and additional resins, plasticizers

and stabilizers which meet or exceed the requirements of the Corps of Engineers

specifications. Types and dimensions of waterstop shall be those shown in the

project specifications.

Typical Properties

CRD-C 573: 	Tensile Strength 1925 psi – 13.3 MPa

CRD-C 573: 	Ultimate Elongation 402%

CRD-C 571: 	Stiffness in Flexure 775 psi

ASTM D-624: 	Tear Resistance 380 lbs. /in.

ASTM D-1149	Ozone Resistance passed

CRD-C 570: 	Low Temperature - No Cracking, Brittleness (-35°F) or Splitting

CRD-C 572: 	Accelerated Extraction

Ultimate Elongation 366% Par 7.1

Tensile Strength 1825 psi Par 7.1

CRD-C 572: 	Effects of Alkalies Loss in Weight

0.10% Max. Par 7.2

Gain in Weight 0.25% Max.

1/4”

1/2”

12”

3/16”

7/8 ID & 1-1/2” OD

Waterstop • Forming Accessories • Rebar Supports • Mesh Supports • Prestressed Accessories